## Slide 1: ENHANCING CLAYEY SOIL STABILITY USING BIOMASS CHAR

## Slide 2: INTRODUCTION
Organic matter derived from living, or recently living plant and animal, which can be used as fuel is called as biomass
In India, majority of population depends largely upon agriculture as their primary source of income
Following every harvest, a huge amount of biomass is generated. It is mostly discarded as “agro waste”

## Slide 3: OBJECTIVE
To study the characteristics and properties of the soil
To study the properties of the stabilized soil using biomass char.
To find out the optimum content of biomass char to be added for obtaining maximum strength.

## Slide 4: scope
To reduce the environmental impact of disposing biomass as waste
To avoid use of chemical compounds like sodium chloride, calcium chloride, sodium silicate and lime for stabilization of soil

## Slide 5: LITERATURE REVIEW
AUTHORS | TITLE | YEAR | INFERENCE
Nikhilesh S. Trivedi & Sachin A. Mandavgane & Ashish Chaurasia | Characterization and valorization of biomass char: a comparison with biomass ash | 2017 | BMC was tested. In this study six different biomass waste were pyrolyzed at 650 °C and its physical & chemical characteristics were found.
Ablish Kumar Meena R. Ayothiraman | IMPROVEMENT OF SUBGRADE SOIL WITH SHREDDED WASTE TYRE CHIPS | 2011 | Poorly graded silty sand was tested. Tyre chips of size 10*20 mm used. optimum range is found to be 2%.CBR value is increased about 21%

## Slide 6
AUTHORS | TITLE | YEAR | INFERENCE
Arichandran.M Harichandran.S.M.K | Stabilization of soft soil using rubber tyre an industrial waste(IJCE) | 2017 | Red soil was tested.shredded tyre of size 15*30 mm is used.author found considerable increase in strength of soil.
Ghatge Sandeep Hambirao Dr.P.G.Rakaraddi | Soil Stabilization Using Waste Shredded Rubber Tyre Chips (IOSR-JMCE) | 2014 | black cotton soil was tested. Tyre waste of 5%,10%,15%and cement of 2%,4% are used. He finally found optimum range of tyre as 5%and cement as 4%.

## Slide 7
AUTHORS | TITLE | YEAR | INFERENCE
Sharma et al. | Stabilization of a Clayey Soil with Fly Ash and Lime: A Micro Level Investigation | 2012 | Addition of fly ash and lime increases strength of soil. The unconfined compressive strength and CBR value increased by addition of fly ash and lime. Addition of fly ash also improved the geotechnical properties of the soil.
Sridharan | Physical and Compaction Behavior of Clay Soil-Fly Ash Mixtures. | 2013 | The liquid limits, compaction characteristics and swelling potential of expansive clay soil–fly ash mixtures are significantly improved. Furthermore, compressibility characteristics of the expansive soil are improved with the addition of fly ash.

## Slide 8: METHODOLOGY
Literature Study
Determination of soil characteristics
Adding BMC in 2.5%,5%,7.5%,10%
Collection of soil sample
Tests on stabilized soil
Interpreting the results

## Slide 9: Laboratory Tests
For sample soil:
  Specific Gravity
  Liquid Limit
  Plastic Limit
  Standard Proctor Compaction test
  Unconfined Compressive Strength(UCC)
  California Bearing Ratio(CBR)
For stabilized soil:
  Standard Proctor Compaction test
  Unconfined Compressive Strength(UCC)
  California Bearing Ratio(CBR)

## Slide 10: Collection of sample
The Biomass sample used in this stabilization process was collected from Tambaram (Tamil Nadu).
Biomass char wastes are collected and made into powder in laboratory
Bio char is a carbon-rich solid that is derived from biomass (organic matter from plants ) that is heated in a limited oxygen environment.
Charcoal is also a carbon-rich solid that is derived from biomass in a similar manner

## Slide 11: PROXIMATE ANALYSIS OF BIO CHAR
S.NO | TEST PARAMETERS | RESULTS(%) | METHOD OF TESTING
1 | MOISTURE | 8.51 | 
2 | VOLATILE MATTER | 13.6 | IS: 1350 part 1
3 | ASH CONTENT | 56.5 | 
4 | FIXED CARBON | 21.4 | 

## Slide 12: SOIL CLASSIFICATION
Specific gravity = 2.73
Liquid limit = 40%
Plastic limit = 10%
Plasticity index = 30%
As per IS Plasticity chart as LL is between 35%-50% & PL>10%. Hence soil is found to be CI-soil
Liquid Limit Apparatus
Plastic limit threads
Specific gravity bottle

## Slide 13: A-line graph

## Slide 14: PROPORTIONS SELECTED
MATERIAL | TRAIL-1 | TRAIL-2 | TRAIL-3 | TRAIL-4 | TRAIL-5
% OF SOIL | 100 | 97.5 | 95 | 92.5 | 90
% OF BMC | 0 | 2.5 | 5 | 7.5 | 10

## Slide 15: STANDARD PROCTOR COMPACTION TEST RESULT
Soil | Water Content (%) | Dry Density (g/cc)
Virgin Soil | 12 | 1.508
Soil+2.5% BMC | 10 | 1.550
Soil+ 5% BMC | 10 | 1.678
Soil+7.5% BMC | 10 | 1.455
Soil+10% BMC | 10 | 1.431

## Slide 16: COMPACTION TEST RESULT
In the compaction test it is very clear that as the percentage of powdered BMC increases the dry density.
This is mainly because of the light weight property of BMC.
Thus the max dry density of stabilized soil is 1.678g/cc & optimum moisture content is 10%
Chart: 
| 8 | 10 | 12
virgin soil | 1.446 | 1.508 | 1.474
2.5% BMC | 1.359 | 1.55 | 1.358
5% BMC | 1.518 | 1.658 | 1.58
7.5% BMC | 1.318 | 1.455 | 1.319
10% BMC | 1.304 | 1.431 | 1.204
Water content(%)
Dry density(g/cc)

## Slide 17: UCC TEST RESULT
SOIL | UNCONFINED STRENGTH(kg/cm2)
VIRGIN SOIL | 1.215
SOIL+2.5% BMC | 1.270
SOIL+ 5% BMC | 1.568
SOIL+7.5% BMC | 1.368
SOIL+10% BMC | 1.223

## Slide 18: UCC Results
The UCC value increases with increase in BMC content up to 5%.
Thus the unconfined strength of the stabilized clay soil is 1.568kg/cm2
The consistency of clay is stiff as qu lies between 100 to 200 kN/m3
Chart: 
| VIRGIN SOIL | STABILIZED SOIL
VIRGIN SOIL | 1.215
2.5% BMC | 1.27
5% BMC | 1.568
7.5% BMC | 1.368
10% BMC | 1.223
UCS (kg/cm 2)

## Slide 19: CBR test result
soil | CBR(%)
Virgin soil | 1.9
Soil+ 5% BMC | 3.28
Soil+10% BMC | 2.18

## Slide 20: CBR results
CBR value also increases with increase in BMC OF 5%.
Hence it will obviously reduce the thickness of the pavement.
The CBR ratio for 5mm exceeds CBR of 2.5mm and CBR is greater than 1.so it fit for subgrade purposes.
Chart: 
| VIRGIN SOIL | STABILIZED SOIL
VIRGIN SOIL | 1.9
5% BMC | 3.28
10% BMC | 2.18
CBR VALUES (%)

## Slide 21: CONCLUSION
On the basis of present experimental study, the following conclusions were drawn.
The properties of the stabilized soil using biomass char were determined.
The optimum amount of BMC waste to be added to stabilize the clayey soil is found to be 5%.
Hence, with this BMC waste in powder form can be added with soil for stabilization process effectively.

## Slide 22: Reference
Purushotham G. Sarvade and Prashant R Shet had done their experiments on “Geotechnical Properties of Problem Clay Stabilized with Crumb Rubber Powder”. Bonfring International Journal of Industrial Engineering and Management Science, Vol. 2, No. 4, December 2012.
Nadgouda, K.A. and Hegde, R.A. had done their experiments on The “Effect of Lime Stabilization on Properties of Black Cotton Soil”. Indian Geotechnical Conference – 2010, GEOtrendz December 16–18, 2010
K.V. Madurwar, P.P. Dahale, A.N.Burile “Comparative Study of Black Cotton Soil Stabilization with RBI Grade 81 and Sodium Silicate”. International Journal of Innovative Research in Science, Engineering and Technology Vol. 2, Issue 2, February 2013.
Shiva Prasad.A, P.T.Ravichandran, R.Annadurai, P.R.Kannan Rajkumar “Study on Effect of Crumb Rubber on Behavior of Soil”. International Journal Of Geomatics And Geosciences Volume 4, No 3, 2014.
B.R.K. Sai Ganesh Kumar, R.V.L. Sai Sumedha, U. Pradeep, K. Gowtham Kumar, P. Padmanabha Reddy “ Subgrade Strengthening Of Roads On Black Cotton Soil Using Quarry Dust”. International Journal of Research in Engineering and Technology eISSN: 2319-1163 | pISSN: 2321-7308
Mohamed A. Shahin and Liao S. Hong “Utilization of Shredded Rubber Tires for Cement-Stabilized Soft Clays”.
Shiva Prasad.A, P.T.Ravichandran, R.Annadurai, P.R.Kannan Rajkumar “ Study on Effect of Crumb Rubber on Behavior of Soil” International Journal of Geomatics and Geosciences Volume 4, No 3, 2014.
Ghatge Sandeep Hambirao,Dr.P.G.Rakaraddi “Soil Stabilization Using Waste Shredded Rubber Tyre Chips”. IOSR Journal of Mechanical and Civil Engineering (IOSR-JMCE) e-ISSN: 2278-1684,p-ISSN: 2320-334X, Volume 11, Issue 1 Ver. V (Feb. 2014)
Kavish S. Mehta, Rutvij J. Sonecha, Parth D. Daxini, Parth B. Ratanpara, Miss Kapilani S. Gaikwad “Analysis of Engineering Properties of Black Cotton Soil & Stabilization Using By Lime.” Miss K S. Gaikwad et al Int. Journal of Engineering Research and Applications,ISSN : 2248-9622, Vol. 4, Issue 5( Version 3), May 2014.

## Slide 23: Journal review
Journal name : “ENHANCING CLAYED SOIL STABILITY USING BIOMASS CHAR”
Submitted on : 28.06.2021
Status : under review.

## Slide 24
THANK
YOU